Critere de filtration : Fil BS (0.2 et 0.25)  MC Method : Both Away

Matière : ST WC CU

| Unit | : | Metric |
| --- | --- | --- |
| Machine | : | W32FB,W53FB(EW100A) |
| Version | : | 8 |
| Wire Type | : | BS |
| Wire Diameter | : | 0.2 |
| Material | : St |  |
| MC. Method | : Both Away |  |
| W. Thickness | : 1~150 |  |
| Angle | : 0~0 |  |
| Nozzle Type | : Laminar |  |
| Nozzle Position | : Away |  |
| M. Condition | : Standard |  |

129

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.2 |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 1 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1016 | E1017 | E1018 | E1019 |  | E1020 |  |  |  |  |  |  |  |
| Roughing | 0.1100 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.1350 | 0.1050 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.1470 | 0.1170 | 0.1050 |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.1520 | 0.1220 | 0.1100 | 0.1050 |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.1540 | 0.1240 | 0.1120 | 0.1070 |  | 0.1070 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.1670 | 0.1370 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1170 | 0.1050 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.1720 | 0.1420 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1220 | 0.1100 | 0.1050 |  |  |  |  |  |  |  |  |  |
| +1 Finish 3 | 0.1740 | 0.1440 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1240 | 0.1120 | 0.1070 |  | 0.1070 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 8.000~11.000 | 10.800~14.900 | 10.800~14.900 | 15.000 |  | 12.000 |  |  |  |  |  |  |  |
| ServoLamp | 8~11 | 6~9 | 6~9 | 4~6 |  | 3~5 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 16 | 8~11 | 7~8 | 3~4 |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.19 | 1.06 ~1.45 | 0.92 ~1.06 | 0.38 ~0.50 |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 3 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1026 | E1027 | E1028 | E1029 |  | E1030 |  |  |  |  |  |  |  |
| Roughing | 0.1200 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.1450 | 0.1050 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.1580 | 0.1180 | 0.1060 |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.1620 | 0.1220 | 0.1100 | 0.1040 |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.1640 | 0.1240 | 0.1120 | 0.1060 |  | 0.1060 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.1780 | 0.1380 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1180 | 0.1060 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.1820 | 0.1420 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1220 | 0.1100 | 0.1040 |  |  |  |  |  |  |  |  |  |
| +1 Finish 3 | 0.1840 | 0.1440 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1240 | 0.1120 | 0.1060 |  | 0.1060 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 6.600~9.000 | 9.600~13.200 | 9.000~12.300 | 15.000 |  | 12.000 |  |  |  |  |  |  |  |
| ServoLamp | 8~11 | 7~9 | 5~7 | 3~5 |  | 3~5 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

130

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.2 |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 5 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1036 | E1037 | E1038 | E1039 |  | E1040 |  |  |  |  |  |  |  |
| Roughing | 0.1200 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.1470 | 0.1050 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.1560 | 0.1140 | 0.1020 |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.1610 | 0.1190 | 0.1070 | 0.1050 |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.1630 | 0.1210 | 0.1090 | 0.1070 |  | 0.1070 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.1760 | 0.1340 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1140 | 0.1020 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.1810 | 0.1390 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1190 | 0.1070 | 0.1050 |  |  |  |  |  |  |  |  |  |
| +1 Finish 3 | 0.1830 | 0.1410 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1210 | 0.1090 | 0.1070 |  | 0.1070 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 5.400~7.500 | 7.400~10.200 | 8.400~11.600 | 15.000 |  | 10.000 |  |  |  |  |  |  |  |
| ServoLamp | 5~7 | 7~9 | 2~4 | 2~4 |  | 3~5 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 13 | 7~8 | 3~4 |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.78 | 0.92 ~1.06 | 0.38 ~0.50 |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 10 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1046 | E1047 | E1048 | E1049 |  | E1050 |  |  |  |  |  |  |  |
| Roughing | 0.1280 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.1670 | 0.1060 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.1760 | 0.1150 | 0.1040 |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.1840 | 0.1230 | 0.1120 | 0.1040 |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.1860 | 0.1250 | 0.1140 | 0.1060 |  | 0.1040 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.1990 | 0.1380 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1150 | 0.1040 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2070 | 0.1460 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1230 | 0.1120 | 0.1040 |  |  |  |  |  |  |  |  |  |
| +1 Finish 3 | 0.2090 | 0.1480 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1250 | 0.1140 | 0.1060 |  | 0.1040 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 5.300~5.500 | 5.100~6.600 | 8.400~10.500 | 8.100~8.180 |  | 6.100~6.130 |  |  |  |  |  |  |  |
| ServoLamp | 4~5 | 6~7 | 0~1 | 10~12 |  | 10~12 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 18~20 | 10~12 | 7~8 | 3~4 |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.47 ~2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

131

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.2 |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 15 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1056 | E1057 | E1058 | E1059 |  | E1060 |  |  |  |  |  |  |  |
| Roughing | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.1670 | 0.1060 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.1770 | 0.1160 | 0.1050 |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.1840 | 0.1230 | 0.1120 | 0.1040 |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.1860 | 0.1250 | 0.1140 | 0.1060 |  | 0.1040 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2000 | 0.1390 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1160 | 0.1050 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2070 | 0.1460 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1230 | 0.1120 | 0.1040 |  |  |  |  |  |  |  |  |  |
| +1 Finish 3 | 0.2090 | 0.1480 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1250 | 0.1140 | 0.1060 |  | 0.1040 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 3.800~4.000 | 3.700~5.300 | 5.400~8.400 | 8.100~8.180 |  | 4.600~6.100 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 6~7 | 0~1 | 10~11 |  | 8~9 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 18~20 | 10~12 | 7~8 | 3~4 |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.47 ~2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 20 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1066 | E1067 | E1068 | E1069 |  | E1070 |  |  |  |  |  |  |  |
| Roughing | 0.1340 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.1700 | 0.1090 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.1780 | 0.1170 | 0.1060 |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.1840 | 0.1230 | 0.1120 | 0.1040 |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.1860 | 0.1250 | 0.1140 | 0.1060 |  | 0.1040 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2010 | 0.1400 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1170 | 0.1060 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2070 | 0.1460 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1230 | 0.1120 | 0.1040 |  |  |  |  |  |  |  |  |  |
| +1 Finish 3 | 0.2090 | 0.1480 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1250 | 0.1140 | 0.1060 |  | 0.1040 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 2.800~3.000 | 2.800~3.400 | 5.500~7.500 | 6.000~6.500 |  | 4.700~5.700 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 6~7 | 0~1 | 7~8 |  | 5~6 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 18~20 | 10~12 | 7~8 | 3~4 |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.47 ~2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

132

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.2 |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 25 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1076 | E1077 | E1078 | E1079 |  | E1080 |  |  |  |  |  |  |  |
| Roughing | 0.1360 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.1710 | 0.1100 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.1780 | 0.1170 | 0.1060 |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.1840 | 0.1230 | 0.1120 | 0.1040 |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.1860 | 0.1250 | 0.1140 | 0.1060 |  | 0.1040 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2010 | 0.1400 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1170 | 0.1060 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2070 | 0.1460 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1230 | 0.1120 | 0.1040 |  |  |  |  |  |  |  |  |  |
| +1 Finish 3 | 0.2090 | 0.1480 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1250 | 0.1140 | 0.1060 |  | 0.1040 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 2.200~2.400 | 2.400~3.000 | 5.100~6.700 | 6.000 |  | 4.400~4.500 |  |  |  |  |  |  |  |
| ServoLamp | 2~3 | 5~6 | 0~1 | 6~7 |  | 4~5 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 18~20 | 10~12 | 7~8 | 3~4 |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.47 ~2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 30 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1086 | E1087 | E1088 | E1089 |  | E1090 |  |  |  |  |  |  |  |
| Roughing | 0.1370 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.1690 | 0.1070 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.1760 | 0.1140 | 0.1060 |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.1840 | 0.1220 | 0.1140 | 0.1050 |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.1850 | 0.1230 | 0.1150 | 0.1060 |  | 0.1040 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2020 | 0.1400 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1140 | 0.1060 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2100 | 0.1480 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1220 | 0.1140 | 0.1050 |  |  |  |  |  |  |  |  |  |
| +1 Finish 3 | 0.2110 | 0.1490 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1230 | 0.1150 | 0.1060 |  | 0.1040 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 1.900~2.200 | 3.000~4.500 | 4.700~8.000 | 6.000 |  | 4.400~4.500 |  |  |  |  |  |  |  |
| ServoLamp | 3~5 | 6~7 | 0~1 | 6~7 |  | 4~5 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

133

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.2 |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 40 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1096 | E2092 | E2093 | E2094 |  | E2095 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1400 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15(D) | 0.1700 | 0.1080 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8(D) | 0.1800 | 0.1180 | 0.1040 |  |  |  |  |  |  |  |  |  |  |
| Finish 4(D) | 0.1890 | 0.1270 | 0.1130 | 0.1050 |  |  |  |  |  |  |  |  |  |
| Finish 3(D) | 0.1910 | 0.1290 | 0.1150 | 0.1070 |  | 0.1050 |  |  |  |  |  |  |  |
| +1 Finish 8(D) | 0.2060 | 0.1440 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1180 | 0.1040 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4(D) | 0.2150 | 0.1530 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1270 | 0.1130 | 0.1050 |  |  |  |  |  |  |  |  |  |
| +1 Finish 3(D) | 0.2170 | 0.1550 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1290 | 0.1150 | 0.1070 |  | 0.1050 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 1.500~1.700 | 2.300~3.600 | 2.700~3.300 | 6.000 |  | 3.000~3.400 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 6~7 | 0~1 | 3~4 |  | 3~5 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 40 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1096 | E1097 | E1098 | E1099 |  | E1100 |  |  |  |  |  |  |  |
| Roughing | 0.1400 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.1700 | 0.1080 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.1800 | 0.1180 | 0.1040 |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.1890 | 0.1270 | 0.1130 | 0.1050 |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.1910 | 0.1290 | 0.1150 | 0.1070 |  | 0.1050 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2060 | 0.1440 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1180 | 0.1040 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2150 | 0.1530 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1270 | 0.1130 | 0.1050 |  |  |  |  |  |  |  |  |  |
| +1 Finish 3 | 0.2170 | 0.1550 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1290 | 0.1150 | 0.1070 |  | 0.1050 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 1.500~1.700 | 2.300~3.600 | 2.700~3.300 | 6.000 |  | 3.000~3.400 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 6~7 | 0~1 | 3~4 |  | 3~5 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

134

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.2 |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 50 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1106 | E2102 | E2103 | E2104 |  | E2105 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1420 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15(D) | 0.1720 | 0.1100 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8(D) | 0.1810 | 0.1190 | 0.1050 |  |  |  |  |  |  |  |  |  |  |
| Finish 4(D) | 0.1890 | 0.1270 | 0.1130 | 0.1050 |  |  |  |  |  |  |  |  |  |
| Finish 3(D) | 0.1910 | 0.1290 | 0.1150 | 0.1070 |  | 0.1050 |  |  |  |  |  |  |  |
| +1 Finish 8(D) | 0.2070 | 0.1450 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1190 | 0.1050 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4(D) | 0.2150 | 0.1530 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1270 | 0.1130 | 0.1050 |  |  |  |  |  |  |  |  |  |
| +1 Finish 3(D) | 0.2170 | 0.1550 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1290 | 0.1150 | 0.1070 |  | 0.1050 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 1.100~1.300 | 1.900~2.400 | 2.500~3.000 | 6.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 5~6 | 0~1 | 2~3 |  | 2~3 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 50 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1106 | E1107 | E1108 | E1109 |  | E1110 |  |  |  |  |  |  |  |
| Roughing | 0.1420 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.1720 | 0.1100 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.1810 | 0.1190 | 0.1050 |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.1890 | 0.1270 | 0.1130 | 0.1050 |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.1910 | 0.1290 | 0.1150 | 0.1070 |  | 0.1050 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2070 | 0.1450 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1190 | 0.1050 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2150 | 0.1530 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1270 | 0.1130 | 0.1050 |  |  |  |  |  |  |  |  |  |
| +1 Finish 3 | 0.2170 | 0.1550 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1290 | 0.1150 | 0.1070 |  | 0.1050 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 1.100~1.300 | 1.900~2.400 | 2.500~3.000 | 6.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 5~6 | 0~1 | 2~3 |  | 2~3 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

135

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.2 |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 60 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1116 | E2112 | E2113 | E2114 |  | E2115 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1410 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15(D) | 0.1720 | 0.1100 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8(D) | 0.1800 | 0.1180 | 0.1050 |  |  |  |  |  |  |  |  |  |  |
| Finish 4(D) | 0.1870 | 0.1250 | 0.1120 | 0.1040 |  |  |  |  |  |  |  |  |  |
| Finish 3(D) | 0.1890 | 0.1270 | 0.1140 | 0.1060 |  | 0.1050 |  |  |  |  |  |  |  |
| +1 Finish 8(D) | 0.2060 | 0.1440 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1180 | 0.1050 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4(D) | 0.2130 | 0.1510 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1250 | 0.1120 | 0.1040 |  |  |  |  |  |  |  |  |  |
| +1 Finish 3(D) | 0.2150 | 0.1530 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1270 | 0.1140 | 0.1060 |  | 0.1050 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.800~1.000 | 1.600~2.100 | 1.800~3.300 | 5.900~6.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 5~6 | 0~1 | 2~3 |  | 1~2 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 60 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1116 | E1117 | E1118 | E1119 |  | E1120 |  |  |  |  |  |  |  |
| Roughing | 0.1410 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.1720 | 0.1100 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.1800 | 0.1180 | 0.1050 |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.1870 | 0.1250 | 0.1120 | 0.1040 |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.1890 | 0.1270 | 0.1140 | 0.1060 |  | 0.1050 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2060 | 0.1440 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1180 | 0.1050 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2130 | 0.1510 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1250 | 0.1120 | 0.1040 |  |  |  |  |  |  |  |  |  |
| +1 Finish 3 | 0.2150 | 0.1530 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1270 | 0.1140 | 0.1060 |  | 0.1050 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.800~1.000 | 1.600~2.100 | 1.800~3.300 | 5.900~6.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 5~6 | 0~1 | 2~3 |  | 1~2 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

136

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.2 |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 70 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1186 | E2182 | E2183 | E2184 |  | E2185 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1490 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15(D) | 0.1800 | 0.1100 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8(D) | 0.1860 | 0.1160 | 0.1040 |  |  |  |  |  |  |  |  |  |  |
| Finish 4(D) | 0.1940 | 0.1240 | 0.1120 | 0.1040 |  |  |  |  |  |  |  |  |  |
| Finish 3(D) | 0.1950 | 0.1250 | 0.1130 | 0.1050 |  | 0.1040 |  |  |  |  |  |  |  |
| +1 Finish 8(D) | 0.2120 | 0.1420 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1160 | 0.1040 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4(D) | 0.2200 | 0.1500 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1240 | 0.1120 | 0.1040 |  |  |  |  |  |  |  |  |  |
| +1 Finish 3(D) | 0.2210 | 0.1510 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1250 | 0.1130 | 0.1050 |  | 0.1040 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.700~0.900 | 1.500~2.000 | 1.600~3.100 | 6.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 4~5 | 0~1 | 2~3 |  | 1~2 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 70 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1186 | E1187 | E1188 | E1189 |  | E1190 |  |  |  |  |  |  |  |
| Roughing | 0.1490 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.1800 | 0.1100 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.1860 | 0.1160 | 0.1040 |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.1940 | 0.1240 | 0.1120 | 0.1040 |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.1950 | 0.1250 | 0.1130 | 0.1050 |  | 0.1040 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2120 | 0.1420 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1160 | 0.1040 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2200 | 0.1500 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1240 | 0.1120 | 0.1040 |  |  |  |  |  |  |  |  |  |
| +1 Finish 3 | 0.2210 | 0.1510 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1250 | 0.1130 | 0.1050 |  | 0.1040 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.700~0.900 | 1.500~2.000 | 1.600~3.100 | 6.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 4~5 | 0~1 | 2~3 |  | 1~2 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

137

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.2 |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 80 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1126 | E2122 | E2123 | E2124 |  | E2125 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1450 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15(D) | 0.1780 | 0.1080 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8(D) | 0.1850 | 0.1150 | 0.1040 |  |  |  |  |  |  |  |  |  |  |
| Finish 4(D) | 0.1920 | 0.1220 | 0.1110 | 0.1040 |  |  |  |  |  |  |  |  |  |
| Finish 3(D) | 0.1940 | 0.1240 | 0.1130 | 0.1060 |  | 0.1050 |  |  |  |  |  |  |  |
| +1 Finish 8(D) | 0.2110 | 0.1410 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1150 | 0.1040 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4(D) | 0.2180 | 0.1480 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1220 | 0.1110 | 0.1040 |  |  |  |  |  |  |  |  |  |
| +1 Finish 3(D) | 0.2200 | 0.1500 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1240 | 0.1130 | 0.1060 |  | 0.1050 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.500~0.700 | 1.400~1.900 | 2.100~3.600 | 5.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 4~5 | 0~1 | 2~3 |  | 1~2 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 80 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1126 | E1127 | E1128 | E1129 |  | E1130 |  |  |  |  |  |  |  |
| Roughing | 0.1450 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.1780 | 0.1080 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.1850 | 0.1150 | 0.1040 |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.1920 | 0.1220 | 0.1110 | 0.1040 |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.1940 | 0.1240 | 0.1130 | 0.1060 |  | 0.1050 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2110 | 0.1410 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1150 | 0.1040 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2180 | 0.1480 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1220 | 0.1110 | 0.1040 |  |  |  |  |  |  |  |  |  |
| +1 Finish 3 | 0.2200 | 0.1500 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1240 | 0.1130 | 0.1060 |  | 0.1050 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.500~0.700 | 1.400~1.900 | 2.100~3.600 | 5.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 4~5 | 0~1 | 2~3 |  | 1~2 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

138

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.2 |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 100 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1136 | E2132 | E2133 | E2134 |  | E2135 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1450 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15(D) | 0.1720 | 0.1100 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8(D) | 0.1790 | 0.1170 | 0.1050 |  |  |  |  |  |  |  |  |  |  |
| Finish 5(D) | 0.1860 | 0.1240 | 0.1120 | 0.1050 |  |  |  |  |  |  |  |  |  |
| Finish 4(D) | 0.1880 | 0.1260 | 0.1140 | 0.1070 |  | 0.1060 |  |  |  |  |  |  |  |
| +1 Finish 8(D) | 0.2020 | 0.1400 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1170 | 0.1050 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 5(D) | 0.2090 | 0.1470 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1240 | 0.1120 | 0.1050 |  |  |  |  |  |  |  |  |  |
| +1 Finish 4(D) | 0.2110 | 0.1490 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1260 | 0.1140 | 0.1070 |  | 0.1060 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.300~0.400 | 0.900~1.200 | 2.800~3.600 | 5.150~5.200 |  | 5.150~5.200 |  |  |  |  |  |  |  |
| ServoLamp | 3~4 | 4~5 | 8~10 | 6~7 |  | 5~6 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 4~5 |  | 3~4 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.50 ~0.63 |  | 0.38 ~0.50 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 100 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1136 | E1137 | E1138 | E1139 |  | E1140 |  |  |  |  |  |  |  |
| Roughing | 0.1450 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.1720 | 0.1100 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.1790 | 0.1170 | 0.1050 |  |  |  |  |  |  |  |  |  |  |
| Finish 5 | 0.1860 | 0.1240 | 0.1120 | 0.1050 |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.1880 | 0.1260 | 0.1140 | 0.1070 |  | 0.1060 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2020 | 0.1400 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1170 | 0.1050 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 5 | 0.2090 | 0.1470 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1240 | 0.1120 | 0.1050 |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2110 | 0.1490 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1260 | 0.1140 | 0.1070 |  | 0.1060 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.300~0.400 | 1.000~1.200 | 3.200~4.000 | 4.900~5.100 |  | 5.000~5.200 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 3~4 | 4~7 | 4~5 |  | 4~5 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 4~5 |  | 3~4 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.50 ~0.63 |  | 0.38 ~0.50 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

139

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.2 |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 125 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1146 | E2142 | E2143 | E2144 |  | E2145 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1450 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15(D) | 0.1720 | 0.1100 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8(D) | 0.1790 | 0.1170 | 0.1050 |  |  |  |  |  |  |  |  |  |  |
| Finish 5(D) | 0.1860 | 0.1240 | 0.1120 | 0.1050 |  |  |  |  |  |  |  |  |  |
| Finish 4(D) | 0.1880 | 0.1260 | 0.1140 | 0.1070 |  | 0.1060 |  |  |  |  |  |  |  |
| +1 Finish 8(D) | 0.2020 | 0.1400 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1170 | 0.1050 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 5(D) | 0.2090 | 0.1470 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1240 | 0.1120 | 0.1050 |  |  |  |  |  |  |  |  |  |
| +1 Finish 4(D) | 0.2110 | 0.1490 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1260 | 0.1140 | 0.1070 |  | 0.1060 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.210~0.300 | 0.900~1.200 | 2.000~2.500 | 3.600~4.000 |  | 3.100~3.300 |  |  |  |  |  |  |  |
| ServoLamp | 1~2 | 3~4 | 4~6 | 5~6 |  | 4~5 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 4~5 |  | 3~4 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.50 ~0.63 |  | 0.38 ~0.50 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 125 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1146 | E1147 | E1148 | E1149 |  | E1150 |  |  |  |  |  |  |  |
| Roughing | 0.1450 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.1720 | 0.1100 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.1790 | 0.1170 | 0.1050 |  |  |  |  |  |  |  |  |  |  |
| Finish 5 | 0.1860 | 0.1240 | 0.1120 | 0.1050 |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.1880 | 0.1260 | 0.1140 | 0.1070 |  | 0.1060 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2020 | 0.1400 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1170 | 0.1050 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 5 | 0.2090 | 0.1470 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1240 | 0.1120 | 0.1050 |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2110 | 0.1490 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1260 | 0.1140 | 0.1070 |  | 0.1060 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.210~0.300 | 0.850~1.150 | 2.300~3.000 | 4.200~4.600 |  | 4.000~4.300 |  |  |  |  |  |  |  |
| ServoLamp | 1~2 | 3~4 | 3~4 | 4~5 |  | 3~4 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 4~5 |  | 3~4 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.50 ~0.63 |  | 0.38 ~0.50 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

140

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.2 |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 150 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1156 | E2152 | E2153 | E2154 |  | E2155 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1450 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15(D) | 0.1720 | 0.1100 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8(D) | 0.1800 | 0.1180 | 0.1060 |  |  |  |  |  |  |  |  |  |  |
| Finish 5(D) | 0.1860 | 0.1240 | 0.1120 | 0.1050 |  |  |  |  |  |  |  |  |  |
| Finish 4(D) | 0.1880 | 0.1260 | 0.1140 | 0.1070 |  | 0.1060 |  |  |  |  |  |  |  |
| +1 Finish 8(D) | 0.2030 | 0.1410 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1180 | 0.1060 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 5(D) | 0.2090 | 0.1470 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1240 | 0.1120 | 0.1050 |  |  |  |  |  |  |  |  |  |
| +1 Finish 4(D) | 0.2110 | 0.1490 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1260 | 0.1140 | 0.1070 |  | 0.1060 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.170~0.220 | 0.300~1.000 | 2.000~2.300 | 2.400~2.700 |  | 2.400~2.700 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 3~4 | 4~8 | 4~5 |  | 3~4 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 4~5 |  | 3~4 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.50 ~0.63 |  | 0.38 ~0.50 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 150 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1156 | E1157 | E1158 | E1159 |  | E1160 |  |  |  |  |  |  |  |
| Roughing | 0.1450 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.1720 | 0.1100 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.1800 | 0.1180 | 0.1060 |  |  |  |  |  |  |  |  |  |  |
| Finish 5 | 0.1860 | 0.1240 | 0.1120 | 0.1050 |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.1880 | 0.1260 | 0.1140 | 0.1070 |  | 0.1060 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2030 | 0.1410 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1180 | 0.1060 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 5 | 0.2090 | 0.1470 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1240 | 0.1120 | 0.1050 |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2110 | 0.1490 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1260 | 0.1140 | 0.1070 |  | 0.1060 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.170~0.220 | 0.600~1.100 | 2.200~3.500 | 3.800~4.400 |  | 3.100~3.300 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 3~4 | 4~6 | 3~4 |  | 3~4 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 4~5 |  | 3~4 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.50 ~0.63 |  | 0.38 ~0.50 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

141

| Unit | : | Metric |
| --- | --- | --- |
| Machine | : | W32FB,W53FB(EW100A) |
| Version | : | 8 |
| Wire Type | : | BS |
| Wire Diameter | : | 0.2 |
| Material | : Cu |  |
| MC. Method | : Both Away |  |
| W. Thickness | : 5~60 |  |
| Angle | : 0~0 |  |
| Nozzle Type | : Laminar |  |
| Nozzle Position | : Away |  |
| M. Condition | : Standard |  |

191

| Unit | Machine |  | Version |  | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.2 |  |  |  | Cu |  | Both Away |  |  |
| Thickness (mm) | 5 |  |  |  |  |  | 10 |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  | 0 |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd |  |  |  | 1st |  |  | 2nd | 3rd |  |  |  |
| ENo | E5636 | E5637 | E5638 |  |  |  | E5646 |  |  | E5647 | E5648 |  |  |  |
| Roughing | 0.1420 |  |  |  |  |  | 0.1480 |  |  |  |  |  |  |  |
| 2nd 10 | 0.1660 | 0.1090 |  |  |  |  | 0.1660 |  |  | 0.1080 |  |  |  |  |
| Finish 4 | 0.1710 | 0.1140 | 0.1070 |  |  |  | 0.1720 |  |  | 0.1140 | 0.1050 |  |  |  |
| +1 Finish 4 | 0.1910 | 0.1340 |  |  |  |  | 0.1920 |  |  | 0.1340 |  |  |  |  |
|  |  | 0.1140 | 0.1070 |  |  |  |  |  |  | 0.1140 | 0.1050 |  |  |  |
| HValue | V-Corner |  |  |  |  |  | V-Corner |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - |  |  |  | - |  |  | - | - |  |  |  |
| PressureL (MPa) | - | - | - |  |  |  | - |  |  | - | - |  |  |  |
| Rem. R. (mm/min) | 7.900~9.700 | 13.400~16.400 | 20.000 |  |  |  | 7.000~8.500 |  |  | 13.800~16.800 | 20.000 |  |  |  |
| ServoLamp | 6~8 | 7~9 | 7~9 |  |  |  | 6~8 |  |  | 9~10 | 7~8 |  |  |  |
| SparkLamp | 12 | 12 | - |  |  |  | 12 |  |  | 12 | - |  |  |  |
| SF1 (µmRz) | 18 | 10 | 3~4 |  |  |  | 18 |  |  | 10 | 3~4 |  |  |  |
| SF2 (µmRa) | 2.47 | 1.32 | 0.38 ~0.50 |  |  |  | 2.47 |  |  | 1.32 | 0.38 ~0.50 |  |  |  |
| AR (mm) | - | - | - |  |  |  | - |  |  | - | - |  |  |  |
| Thickness (mm) | 15 |  |  |  |  |  | 20 |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  | 0 |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd |  |  |  | 1st |  |  | 2nd | 3rd |  |  |  |
| ENo | E5656 | E5657 | E5658 |  |  |  | E5666 |  |  | E5667 | E5668 |  |  |  |
| Roughing | 0.1530 |  |  |  |  |  | 0.1530 |  |  |  |  |  |  |  |
| 2nd 10 | 0.1690 | 0.1070 |  |  |  |  | 0.1720 |  |  | 0.1100 |  |  |  |  |
| Finish 4 | 0.1750 | 0.1130 | 0.1060 |  |  |  | 0.1780 |  |  | 0.1160 | 0.1060 |  |  |  |
| +1 Finish 4 | 0.1950 | 0.1330 |  |  |  |  | 0.1980 |  |  | 0.1360 |  |  |  |  |
|  |  | 0.1130 | 0.1060 |  |  |  |  |  |  | 0.1160 | 0.1060 |  |  |  |
| HValue | V-Corner |  |  |  |  |  | V-Corner |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - |  |  |  | - |  |  | - | - |  |  |  |
| PressureL (MPa) | - | - | - |  |  |  | - |  |  | - | - |  |  |  |
| Rem. R. (mm/min) | 4.800~5.800 | 12.300~15.100 | 20.000 |  |  |  | 4.700~5.700 |  |  | 8.400~10.200 | 15.000 |  |  |  |
| ServoLamp | 6~7 | 9~10 | 6~8 |  |  |  | 5~7 |  |  | 9~10 | 5~8 |  |  |  |
| SparkLamp | 12 | 12 | - |  |  |  | 12 |  |  | 12 | - |  |  |  |
| SF1 (µmRz) | 18 | 10 | 3~4 |  |  |  | 18 |  |  | 10 | 3~4 |  |  |  |
| SF2 (µmRa) | 2.47 | 1.32 | 0.38 ~0.50 |  |  |  | 2.47 |  |  | 1.32 | 0.38 ~0.50 |  |  |  |
| AR (mm) | - | - | - |  |  |  | - |  |  | - | - |  |  |  |
| Thickness (mm) | 25 |  |  |  |  |  | 30 |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  | 0 |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd |  |  |  | 1st |  |  | 2nd | 3rd |  |  |  |
| ENo | E5676 | E5677 | E5678 |  |  |  | E5686 |  |  | E5687 | E5688 |  |  |  |
| Roughing | 0.1580 |  |  |  |  |  | 0.1610 |  |  |  |  |  |  |  |
| 2nd 10 | 0.1760 | 0.1100 |  |  |  |  | 0.1800 |  |  | 0.1110 |  |  |  |  |
| Finish 4 | 0.1800 | 0.1140 | 0.1060 |  |  |  | 0.1860 |  |  | 0.1170 | 0.1060 |  |  |  |
| +1 Finish 4 | 0.2000 | 0.1340 |  |  |  |  | 0.2060 |  |  | 0.1370 |  |  |  |  |
|  |  | 0.1140 | 0.1060 |  |  |  |  |  |  | 0.1170 | 0.1060 |  |  |  |
| HValue | V-Corner |  |  |  |  |  | V-Corner |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - |  |  |  | - |  |  | - | - |  |  |  |
| PressureL (MPa) | - | - | - |  |  |  | - |  |  | - | - |  |  |  |
| Rem. R. (mm/min) | 3.900~4.700 | 7.700~9.500 | 15.000 |  |  |  | 3.300~4.000 |  |  | 5.900~7.000 | 10.000 |  |  |  |
| ServoLamp | 6~7 | 8~9 | 4~5 |  |  |  | 6~7 |  |  | 8~9 | 4~5 |  |  |  |
| SparkLamp | 12 | 12 | - |  |  |  | 12 |  |  | 12 | - |  |  |  |
| SF1 (µmRz) | 18 | 10 | 3~4 |  |  |  | 18 |  |  | 10 | 3~4 |  |  |  |
| SF2 (µmRa) | 2.47 | 1.32 | 0.38 ~0.50 |  |  |  | 2.47 |  |  | 1.32 | 0.38 ~0.50 |  |  |  |
| AR (mm) | - | - | - |  |  |  | - |  |  | - | - |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

192

| Unit | Machine |  | Version |  | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.2 |  |  |  | Cu |  | Both Away |  |  |
| Thickness (mm) | 40 |  |  |  |  |  | 50 |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  | 0 |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd |  |  |  | 1st |  |  | 2nd | 3rd |  |  |  |
| ENo | E5696 | E5697 | E5698 |  |  |  | E5706 |  |  | E5707 | E5708 |  |  |  |
| Roughing | 0.1640 |  |  |  |  |  | 0.1690 |  |  |  |  |  |  |  |
| 2nd 10 | 0.1850 | 0.1130 |  |  |  |  | 0.1900 |  |  | 0.1160 |  |  |  |  |
| Finish 4 | 0.1910 | 0.1190 | 0.1070 |  |  |  | 0.1960 |  |  | 0.1220 | 0.1070 |  |  |  |
| +1 Finish 4 | 0.2110 | 0.1390 |  |  |  |  | 0.2160 |  |  | 0.1420 |  |  |  |  |
|  |  | 0.1190 | 0.1070 |  |  |  |  |  |  | 0.1220 | 0.1070 |  |  |  |
| HValue | V-Corner |  |  |  |  |  | V-Corner |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - |  |  |  | - |  |  | - | - |  |  |  |
| PressureL (MPa) | - | - | - |  |  |  | - |  |  | - | - |  |  |  |
| Rem. R. (mm/min) | 2.300~2.800 | 4.000~4.800 | 10.000 |  |  |  | 1.700~2.100 |  |  | 3.100~3.700 | 10.000 |  |  |  |
| ServoLamp | 5~7 | 8~9 | 1~3 |  |  |  | 5~7 |  |  | 9~10 | 1~3 |  |  |  |
| SparkLamp | 12 | 12 | - |  |  |  | 12 |  |  | 12 | - |  |  |  |
| SF1 (µmRz) | 18 | 10 | 3~4 |  |  |  | 18 |  |  | 10 | 3~4 |  |  |  |
| SF2 (µmRa) | 2.47 | 1.32 | 0.38 ~0.50 |  |  |  | 2.47 |  |  | 1.32 | 0.38 ~0.50 |  |  |  |
| AR (mm) | - | - | - |  |  |  | - |  |  | - | - |  |  |  |
| Thickness (mm) | 60 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd |  |  |  |  |  |  |  |  |  |  |  |
| ENo | E5716 | E5717 | E5718 |  |  |  |  |  |  |  |  |  |  |  |
| Roughing | 0.1730 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10 | 0.1930 | 0.1170 |  |  |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.1980 | 0.1220 | 0.1060 |  |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2180 | 0.1420 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1220 | 0.1060 |  |  |  |  |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - |  |  |  |  |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - |  |  |  |  |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 1.400~1.700 | 2.400~3.000 | 10.000 |  |  |  |  |  |  |  |  |  |  |  |
| ServoLamp | 5~7 | 9~10 | 1~3 |  |  |  |  |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | - |  |  |  |  |  |  |  |  |  |  |  |
| SF1 (µmRz) | 18 | 10 | 3~4 |  |  |  |  |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.47 | 1.32 | 0.38 ~0.50 |  |  |  |  |  |  |  |  |  |  |  |
| AR (mm) | - | - | - |  |  |  |  |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

193

| Unit | : | Metric |
| --- | --- | --- |
| Machine | : | W32FB,W53FB(EW100A) |
| Version | : | 8 |
| Wire Type | : | BS |
| Wire Diameter | : | 0.2 |
| Material | : WC |  |
| MC. Method | : Both Away |  |
| W. Thickness | : 5~60 |  |
| Angle | : 0~0 |  |
| Nozzle Type | : Laminar |  |
| Nozzle Position | : Away |  |
| M. Condition | : Standard |  |

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.2 |  |  | WC |  | Both Away |  |  |
| Thickness (mm) | 5 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1436 | E3437 | E3438 | E3439 |  | E3440 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1210 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10(D) | 0.1560 | 0.1080 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5(D) | 0.1630 | 0.1150 | 0.1090 |  |  |  |  |  |  |  |  |  |  |
| Finish 2(D) | 0.1670 | 0.1190 | 0.1130 | 0.1070 |  |  |  |  |  |  |  |  |  |
| Finish 1.5(D) | 0.1700 | 0.1220 | 0.1160 | 0.1100 |  | 0.1070 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 3.600~4.400 | 4.200~5.600 | 6.900~9.300 | 10.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 6~8 | 3~5 | 5~7 |  | 5~7 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 5 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1436 | E1437 | E1438 | E1439 |  | E1440 |  |  |  |  |  |  |  |
| Roughing | 0.1210 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10 | 0.1560 | 0.1080 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5 | 0.1630 | 0.1150 | 0.1090 |  |  |  |  |  |  |  |  |  |  |
| Finish 2 | 0.1670 | 0.1190 | 0.1130 | 0.1070 |  |  |  |  |  |  |  |  |  |
| Finish 1.5 | 0.1700 | 0.1220 | 0.1160 | 0.1100 |  | 0.1070 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 3.600~4.400 | 4.900~6.700 | 6.800~9.200 | 10.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 6~8 | 3~5 | 5~7 |  | 5~7 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 10 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1446 | E3447 | E3448 | E3449 |  | E3450 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1250 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10(D) | 0.1580 | 0.1060 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5(D) | 0.1680 | 0.1160 | 0.1080 |  |  |  |  |  |  |  |  |  |  |
| Finish 2(D) | 0.1740 | 0.1220 | 0.1140 | 0.1090 |  |  |  |  |  |  |  |  |  |
| Finish 1.5(D) | 0.1750 | 0.1230 | 0.1150 | 0.1100 |  | 0.1070 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 2.700~3.300 | 3.200~4.400 | 4.300~5.800 | 6.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 6~8 | 2~4 | 4~6 |  | 4~6 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

222

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.2 |  |  | WC |  | Both Away |  |  |
| Thickness (mm) | 10 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1446 | E1447 | E1448 | E1449 |  | E1450 |  |  |  |  |  |  |  |
| Roughing | 0.1250 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10 | 0.1580 | 0.1060 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5 | 0.1680 | 0.1160 | 0.1080 |  |  |  |  |  |  |  |  |  |  |
| Finish 2 | 0.1740 | 0.1220 | 0.1140 | 0.1090 |  |  |  |  |  |  |  |  |  |
| Finish 1.5 | 0.1750 | 0.1230 | 0.1150 | 0.1100 |  | 0.1070 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 2.700~3.300 | 3.600~4.800 | 4.400~6.000 | 6.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 6~8 | 2~4 | 4~6 |  | 4~6 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 15 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1456 | E3457 | E3458 | E3459 |  | E3460 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1260 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10(D) | 0.1590 | 0.1060 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5(D) | 0.1700 | 0.1170 | 0.1080 |  |  |  |  |  |  |  |  |  |  |
| Finish 2(D) | 0.1760 | 0.1230 | 0.1140 | 0.1090 |  |  |  |  |  |  |  |  |  |
| Finish 1.5(D) | 0.1770 | 0.1240 | 0.1150 | 0.1100 |  | 0.1070 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 2.300~2.800 | 2.800~3.800 | 2.600~3.500 | 5.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 6~8 | 2~4 | 5~7 |  | 4~6 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 15 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1456 | E1457 | E1458 | E1459 |  | E1460 |  |  |  |  |  |  |  |
| Roughing | 0.1260 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10 | 0.1590 | 0.1060 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5 | 0.1700 | 0.1170 | 0.1080 |  |  |  |  |  |  |  |  |  |  |
| Finish 2 | 0.1760 | 0.1230 | 0.1140 | 0.1090 |  |  |  |  |  |  |  |  |  |
| Finish 1.5 | 0.1770 | 0.1240 | 0.1150 | 0.1100 |  | 0.1070 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 2.300~2.800 | 3.100~4.100 | 2.600~3.600 | 5.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 6~8 | 2~4 | 5~7 |  | 4~6 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

223

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.2 |  |  | WC |  | Both Away |  |  |
| Thickness (mm) | 20 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1466 | E3467 | E3468 | E3469 |  | E3470 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1300 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10(D) | 0.1640 | 0.1070 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5(D) | 0.1760 | 0.1190 | 0.1090 |  |  |  |  |  |  |  |  |  |  |
| Finish 2(D) | 0.1810 | 0.1240 | 0.1140 | 0.1080 |  |  |  |  |  |  |  |  |  |
| Finish 1.5(D) | 0.1820 | 0.1250 | 0.1150 | 0.1090 |  | 0.1070 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 1.600~2.000 | 2.000~2.800 | 2.000~2.600 | 5.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 4~6 | 2~4 | 5~7 |  | 4~6 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 20 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1466 | E1467 | E1468 | E1469 |  | E1470 |  |  |  |  |  |  |  |
| Roughing | 0.1300 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10 | 0.1640 | 0.1070 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5 | 0.1760 | 0.1190 | 0.1090 |  |  |  |  |  |  |  |  |  |  |
| Finish 2 | 0.1810 | 0.1240 | 0.1140 | 0.1080 |  |  |  |  |  |  |  |  |  |
| Finish 1.5 | 0.1820 | 0.1250 | 0.1150 | 0.1090 |  | 0.1070 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 1.600~2.000 | 2.100~2.900 | 2.000~2.800 | 5.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 4~6 | 2~4 | 5~7 |  | 4~6 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 25 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1476 | E3477 | E3478 | E3479 |  | E3480 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1350 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10(D) | 0.1680 | 0.1060 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5(D) | 0.1790 | 0.1170 | 0.1090 |  |  |  |  |  |  |  |  |  |  |
| Finish 2(D) | 0.1820 | 0.1200 | 0.1120 | 0.1060 |  |  |  |  |  |  |  |  |  |
| Finish 1.5(D) | 0.1850 | 0.1230 | 0.1150 | 0.1090 |  | 0.1070 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 1.300~1.500 | 1.400~1.800 | 1.900~2.500 | 4.500 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 4~6 | 6~8 | 4~6 |  | 4~6 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

224

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.2 |  |  | WC |  | Both Away |  |  |
| Thickness (mm) | 25 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1476 | E1477 | E1478 | E1479 |  | E1480 |  |  |  |  |  |  |  |
| Roughing | 0.1350 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10 | 0.1680 | 0.1060 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5 | 0.1790 | 0.1170 | 0.1090 |  |  |  |  |  |  |  |  |  |  |
| Finish 2 | 0.1820 | 0.1200 | 0.1120 | 0.1060 |  |  |  |  |  |  |  |  |  |
| Finish 1.5 | 0.1850 | 0.1230 | 0.1150 | 0.1090 |  | 0.1070 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 1.300~1.500 | 1.500~2.100 | 2.000~2.600 | 4.500 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 4~6 | 6~8 | 4~6 |  | 4~6 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 30 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1486 | E3487 | E3488 | E3489 |  | E3490 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1360 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10(D) | 0.1690 | 0.1070 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5(D) | 0.1800 | 0.1180 | 0.1090 |  |  |  |  |  |  |  |  |  |  |
| Finish 2(D) | 0.1840 | 0.1220 | 0.1130 | 0.1070 |  |  |  |  |  |  |  |  |  |
| Finish 1.5(D) | 0.1870 | 0.1250 | 0.1160 | 0.1100 |  | 0.1080 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 1.200~1.400 | 1.300~1.700 | 1.800~2.400 | 4.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 4~6 | 2~4 | 4~6 |  | 4~6 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 30 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1486 | E1487 | E1488 | E1489 |  | E1490 |  |  |  |  |  |  |  |
| Roughing | 0.1360 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10 | 0.1690 | 0.1070 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5 | 0.1800 | 0.1180 | 0.1090 |  |  |  |  |  |  |  |  |  |  |
| Finish 2 | 0.1840 | 0.1220 | 0.1130 | 0.1070 |  |  |  |  |  |  |  |  |  |
| Finish 1.5 | 0.1870 | 0.1250 | 0.1160 | 0.1100 |  | 0.1080 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 1.200~1.400 | 1.400~1.800 | 1.900~2.500 | 4.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 4~6 | 2~4 | 4~6 |  | 4~6 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

225

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.2 |  |  | WC |  | Both Away |  |  |
| Thickness (mm) | 40 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1496 | E3497 | E3498 | E3499 |  | E3500 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1380 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10(D) | 0.1730 | 0.1100 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5(D) | 0.1850 | 0.1220 | 0.1090 |  |  |  |  |  |  |  |  |  |  |
| Finish 2(D) | 0.1890 | 0.1260 | 0.1130 | 0.1070 |  |  |  |  |  |  |  |  |  |
| Finish 1.5(D) | 0.1900 | 0.1270 | 0.1140 | 0.1080 |  | 0.1060 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.800~1.000 | 0.900~1.300 | 1.400~2.000 | 4.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 5~7 | 4~6 | 2~4 |  | 2~4 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 40 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1496 | E1497 | E1498 | E1499 |  | E1500 |  |  |  |  |  |  |  |
| Roughing | 0.1380 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10 | 0.1730 | 0.1100 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5 | 0.1850 | 0.1220 | 0.1090 |  |  |  |  |  |  |  |  |  |  |
| Finish 2 | 0.1890 | 0.1260 | 0.1130 | 0.1070 |  |  |  |  |  |  |  |  |  |
| Finish 1.5 | 0.1900 | 0.1270 | 0.1140 | 0.1080 |  | 0.1060 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.800~1.000 | 1.000~1.400 | 1.500~2.100 | 4.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 5~7 | 4~6 | 2~4 |  | 2~4 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 50 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1506 | E3507 | E3508 | E3509 |  | E3510 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1390 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10(D) | 0.1750 | 0.1110 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5(D) | 0.1850 | 0.1210 | 0.1080 |  |  |  |  |  |  |  |  |  |  |
| Finish 2(D) | 0.1890 | 0.1250 | 0.1120 | 0.1060 |  |  |  |  |  |  |  |  |  |
| Finish 1.5(D) | 0.1890 | 0.1250 | 0.1120 | 0.1060 |  | 0.1040 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.600~0.800 | 0.900~1.300 | 1.100~1.500 | 4.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 5~7 | 4~6 | 2~4 |  | 2~4 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

226

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.2 |  |  | WC |  | Both Away |  |  |
| Thickness (mm) | 50 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1506 | E1507 | E1508 | E1509 |  | E1510 |  |  |  |  |  |  |  |
| Roughing | 0.1390 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10 | 0.1750 | 0.1110 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5 | 0.1850 | 0.1210 | 0.1080 |  |  |  |  |  |  |  |  |  |  |
| Finish 2 | 0.1890 | 0.1250 | 0.1120 | 0.1060 |  |  |  |  |  |  |  |  |  |
| Finish 1.5 | 0.1890 | 0.1250 | 0.1120 | 0.1060 |  | 0.1040 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.600~0.800 | 1.000~1.400 | 1.000~1.400 | 4.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 5~7 | 4~6 | 2~4 |  | 2~4 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 60 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1516 | E3517 | E3518 | E3519 |  | E3520 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1410 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10(D) | 0.1770 | 0.1120 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5(D) | 0.1870 | 0.1220 | 0.1090 |  |  |  |  |  |  |  |  |  |  |
| Finish 2(D) | 0.1910 | 0.1260 | 0.1130 | 0.1060 |  |  |  |  |  |  |  |  |  |
| Finish 1.5(D) | 0.1910 | 0.1260 | 0.1130 | 0.1060 |  | 0.1040 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.500~0.600 | 0.900~1.300 | 0.900~1.200 | 3.000 |  | 2.500 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 5~7 | 2~4 | 2~3 |  | 3~5 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 60 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1516 | E1517 | E1518 | E1519 |  | E1520 |  |  |  |  |  |  |  |
| Roughing | 0.1410 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10 | 0.1770 | 0.1120 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5 | 0.1870 | 0.1220 | 0.1090 |  |  |  |  |  |  |  |  |  |  |
| Finish 2 | 0.1910 | 0.1260 | 0.1130 | 0.1060 |  |  |  |  |  |  |  |  |  |
| Finish 1.5 | 0.1910 | 0.1260 | 0.1130 | 0.1060 |  | 0.1040 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.500~0.600 | 1.000~1.400 | 0.900~1.300 | 3.000 |  | 2.500 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 5~7 | 2~4 | 2~3 |  | 3~5 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

227

| Unit | : | Metric |
| --- | --- | --- |
| Machine | : | W32FB,W53FB(EW100A) |
| Version | : | 8 |
| Wire Type | : | BS |
| Wire Diameter | : | 0.25 |
| Material | : St |  |
| MC. Method | : Both Away |  |
| W. Thickness | : 1~200 |  |
| Angle | : 0~0 |  |
| Nozzle Type | : Laminar |  |
| Nozzle Position | : Away |  |
| M. Condition | : Standard |  |

291

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS | 0.25 |  |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 1 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1016 | E1017 | E1018 | E1019 |  | E1020 |  |  |  |  |  |  |  |
| Roughing | 0.1480 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.1750 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.1850 | 0.1420 | 0.1320 |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.1890 | 0.1460 | 0.1360 | 0.1330 |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.1900 | 0.1470 | 0.1370 | 0.1340 |  | 0.1320 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 5.400~7.400 | 8.800~12.100 | 8.000~11.000 | 10.000 |  | 15.000 |  |  |  |  |  |  |  |
| ServoLamp | 6~8 | 7~9 | 3~6 | 3~5 |  | 3~5 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 3 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1026 | E1027 | E1028 | E1029 |  | E1030 |  |  |  |  |  |  |  |
| Roughing | 0.1570 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.1850 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.1950 | 0.1420 | 0.1320 |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.2000 | 0.1470 | 0.1370 | 0.1340 |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.2000 | 0.1470 | 0.1370 | 0.1340 |  | 0.1320 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 5.000~6.900 | 8.400~11.600 | 8.000~11.000 | 10.000 |  | 15.000 |  |  |  |  |  |  |  |
| ServoLamp | 7~8 | 7~10 | 2~5 | 3~5 |  | 3~5 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

292

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS | 0.25 |  |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 5 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1036 | E1037 | E1038 | E1039 |  | E1040 |  |  |  |  |  |  |  |
| Roughing | 0.1610 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.1850 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.1950 | 0.1420 | 0.1330 |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.1970 | 0.1440 | 0.1350 | 0.1330 |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.1990 | 0.1460 | 0.1370 | 0.1350 |  | 0.1330 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2110 | 0.1580 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1420 | 0.1330 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2130 | 0.1600 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1440 | 0.1350 | 0.1330 |  |  |  |  |  |  |  |  |  |
| +1 Finish 3 | 0.2150 | 0.1620 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1460 | 0.1370 | 0.1350 |  | 0.1330 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 4.800~6.600 | 7.200~9.900 | 8.000~11.000 | 10.000 |  | 15.000 |  |  |  |  |  |  |  |
| ServoLamp | 6~8 | 7~9 | 3~6 | 3~5 |  | 7~8 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 10 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1046 | E1047 | E1048 | E1049 |  | E1050 |  |  |  |  |  |  |  |
| Roughing | 0.1570 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.1910 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.2000 | 0.1410 | 0.1300 |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.2070 | 0.1480 | 0.1370 | 0.1290 |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.2090 | 0.1500 | 0.1390 | 0.1310 |  | 0.1300 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2220 | 0.1630 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1410 | 0.1300 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2290 | 0.1700 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1480 | 0.1370 | 0.1290 |  |  |  |  |  |  |  |  |  |
| +1 Finish 3 | 0.2310 | 0.1720 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1500 | 0.1390 | 0.1310 |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 5.700~5.900 | 5.100~6.600 | 8.500~11.200 | 11.500~11.700 |  | 7.200~8.700 |  |  |  |  |  |  |  |
| ServoLamp | 3~5 | 6~7 | 0~1 | 11~12 |  | 4~5 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

293

| Unit | Machine |  | Version | Wire |  |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.25 |  |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 15 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  |  | 5th |  |  |  |  |  |  |  |
| ENo | E1056 | E1057 | E1058 | E1059 |  |  | E1060 |  |  |  |  |  |  |  |
| Roughing | 0.1620 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.1910 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.2000 | 0.1410 | 0.1300 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.2070 | 0.1480 | 0.1370 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.2090 | 0.1500 | 0.1390 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2220 | 0.1630 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1410 | 0.1300 |  |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2290 | 0.1700 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1480 | 0.1370 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 3 | 0.2310 | 0.1720 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1500 | 0.1390 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 4.900~5.100 | 3.700~5.300 | 5.900~7.500 | 8.900~10.400 |  |  | 6.000~7.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 6~7 | 0~1 | 9~10 |  |  | 2~3 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 20 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  |  | 5th |  |  |  |  |  |  |  |
| ENo | E1066 | E1067 | E1068 | E1069 |  |  | E1070 |  |  |  |  |  |  |  |
| Roughing | 0.1640 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.1920 | 0.1330 |  |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.2010 | 0.1420 | 0.1310 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.2070 | 0.1480 | 0.1370 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.2090 | 0.1500 | 0.1390 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2230 | 0.1640 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1420 | 0.1310 |  |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2290 | 0.1700 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1480 | 0.1370 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 3 | 0.2310 | 0.1720 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1500 | 0.1390 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 4.000~4.200 | 3.900~4.500 | 5.000~6.000 | 6.300~7.300 |  |  | 4.500~5.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 6~7 | 0~1 | 7~8 |  |  | 1~2 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

294

| Unit | Machine |  | Version | Wire |  |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.25 |  |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 25 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  |  | 5th |  |  |  |  |  |  |  |
| ENo | E1076 | E1077 | E1078 | E1079 |  |  | E1080 |  |  |  |  |  |  |  |
| Roughing | 0.1690 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.1940 | 0.1350 |  |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.2010 | 0.1420 | 0.1310 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.2080 | 0.1490 | 0.1380 | 0.1300 |  |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.2090 | 0.1500 | 0.1390 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2230 | 0.1640 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1420 | 0.1310 |  |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2300 | 0.1710 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1490 | 0.1380 | 0.1300 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 3 | 0.2310 | 0.1720 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1500 | 0.1390 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 3.600~3.800 | 3.400~5.000 | 4.800~5.500 | 6.000~6.500 |  |  | 4.500 |  |  |  |  |  |  |  |
| ServoLamp | 1~2 | 5~6 | 0~1 | 6~7 |  |  | 1~2 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 30 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  |  | 5th |  |  |  |  |  |  |  |
| ENo | E1086 | E2082 | E2083 | E2084 |  |  | E2085 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1700 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15(D) | 0.2050 | 0.1330 |  |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8(D) | 0.2150 | 0.1430 | 0.1300 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 4(D) | 0.2220 | 0.1500 | 0.1370 | 0.1280 |  |  |  |  |  |  |  |  |  |  |
| Finish 3(D) | 0.2250 | 0.1530 | 0.1400 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| +1 Finish 8(D) | 0.2330 | 0.1610 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1430 | 0.1300 |  |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4(D) | 0.2400 | 0.1680 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1500 | 0.1370 | 0.1280 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 3(D) | 0.2430 | 0.1710 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1530 | 0.1400 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 2.900~3.100 | 3.100~4.800 | 3.600~4.000 | 7.200 |  |  | 3.600 |  |  |  |  |  |  |  |
| ServoLamp | 1~2 | 6~7 | 0~1 | 4~5 |  |  | 6~7 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

295

| Unit | Machine |  | Version | Wire |  |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.25 |  |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 30 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  |  | 5th |  |  |  |  |  |  |  |
| ENo | E1086 | E1087 | E1088 | E1089 |  |  | E1090 |  |  |  |  |  |  |  |
| Roughing | 0.1700 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.2050 | 0.1330 |  |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.2150 | 0.1430 | 0.1300 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.2220 | 0.1500 | 0.1370 | 0.1280 |  |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.2250 | 0.1530 | 0.1400 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2330 | 0.1610 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1430 | 0.1300 |  |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2400 | 0.1680 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1500 | 0.1370 | 0.1280 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 3 | 0.2430 | 0.1710 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1530 | 0.1400 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 2.900~3.100 | 3.100~4.800 | 3.600~4.000 | 7.200 |  |  | 3.600 |  |  |  |  |  |  |  |
| ServoLamp | 1~2 | 6~7 | 0~1 | 4~5 |  |  | 6~7 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 40 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  |  | 5th |  |  |  |  |  |  |  |
| ENo | E1096 | E2092 | E2093 | E2094 |  |  | E2095 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1740 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15(D) | 0.2060 | 0.1340 |  |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8(D) | 0.2150 | 0.1430 | 0.1300 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 4(D) | 0.2220 | 0.1500 | 0.1370 | 0.1280 |  |  |  |  |  |  |  |  |  |  |
| Finish 3(D) | 0.2250 | 0.1530 | 0.1400 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| +1 Finish 8(D) | 0.2330 | 0.1610 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1430 | 0.1300 |  |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4(D) | 0.2400 | 0.1680 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1500 | 0.1370 | 0.1280 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 3(D) | 0.2430 | 0.1710 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1530 | 0.1400 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 2.100~2.300 | 2.200~4.500 | 5.300~6.300 | 6.600~7.100 |  |  | 3.200~3.600 |  |  |  |  |  |  |  |
| ServoLamp | 3~5 | 6~7 | 0~1 | 3 |  |  | 5~6 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

296

| Unit | Machine |  | Version | Wire |  |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.25 |  |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 40 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  |  | 5th |  |  |  |  |  |  |  |
| ENo | E1096 | E1097 | E1098 | E1099 |  |  | E1100 |  |  |  |  |  |  |  |
| Roughing | 0.1740 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.2060 | 0.1340 |  |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.2150 | 0.1430 | 0.1300 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.2220 | 0.1500 | 0.1370 | 0.1280 |  |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.2250 | 0.1530 | 0.1400 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2330 | 0.1610 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1430 | 0.1300 |  |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2400 | 0.1680 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1500 | 0.1370 | 0.1280 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 3 | 0.2430 | 0.1710 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1530 | 0.1400 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 2.100~2.300 | 2.200~4.500 | 5.300~6.300 | 6.600~7.100 |  |  | 3.200~3.600 |  |  |  |  |  |  |  |
| ServoLamp | 3~5 | 6~7 | 0~1 | 3 |  |  | 5~6 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 50 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  |  | 5th |  |  |  |  |  |  |  |
| ENo | E1106 | E2102 | E2103 | E2104 |  |  | E2105 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1760 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15(D) | 0.2070 | 0.1350 |  |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8(D) | 0.2160 | 0.1440 | 0.1310 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 4(D) | 0.2220 | 0.1500 | 0.1370 | 0.1280 |  |  |  |  |  |  |  |  |  |  |
| Finish 3(D) | 0.2250 | 0.1530 | 0.1400 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| +1 Finish 8(D) | 0.2340 | 0.1620 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1440 | 0.1310 |  |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4(D) | 0.2400 | 0.1680 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1500 | 0.1370 | 0.1280 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 3(D) | 0.2430 | 0.1710 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1530 | 0.1400 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 1.600~1.800 | 1.900~3.000 | 2.500~3.200 | 6.000 |  |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 5~7 | 0~1 | 2~3 |  |  | 3~4 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

297

| Unit | Machine |  | Version | Wire |  |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.25 |  |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 50 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  |  | 5th |  |  |  |  |  |  |  |
| ENo | E1106 | E1107 | E1108 | E1109 |  |  | E1110 |  |  |  |  |  |  |  |
| Roughing | 0.1760 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.2070 | 0.1350 |  |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.2160 | 0.1440 | 0.1310 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.2220 | 0.1500 | 0.1370 | 0.1280 |  |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.2250 | 0.1530 | 0.1400 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2340 | 0.1620 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1440 | 0.1310 |  |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2400 | 0.1680 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1500 | 0.1370 | 0.1280 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 3 | 0.2430 | 0.1710 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1530 | 0.1400 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 1.600~1.800 | 1.900~3.000 | 2.500~3.200 | 6.000 |  |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 5~7 | 0~1 | 2~3 |  |  | 3~4 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 60 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  |  | 5th |  |  |  |  |  |  |  |
| ENo | E1116 | E2112 | E2113 | E2114 |  |  | E2115 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1790 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15(D) | 0.2090 | 0.1370 |  |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8(D) | 0.2170 | 0.1450 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 4(D) | 0.2230 | 0.1510 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| Finish 3(D) | 0.2250 | 0.1530 | 0.1400 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| +1 Finish 8(D) | 0.2350 | 0.1630 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1450 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4(D) | 0.2410 | 0.1690 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1510 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 3(D) | 0.2430 | 0.1710 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1530 | 0.1400 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 1.300~1.500 | 1.900~2.800 | 1.800~4.000 | 5.900~6.000 |  |  | 2.900~3.000 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 5~7 | 0~1 | 1~2 |  |  | 2~3 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

298

| Unit | Machine |  | Version | Wire |  |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.25 |  |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 60 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  |  | 5th |  |  |  |  |  |  |  |
| ENo | E1116 | E1117 | E1118 | E1119 |  |  | E1120 |  |  |  |  |  |  |  |
| Roughing | 0.1790 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.2090 | 0.1370 |  |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.2170 | 0.1450 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.2230 | 0.1510 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.2250 | 0.1530 | 0.1400 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2350 | 0.1630 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1450 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2410 | 0.1690 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1510 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 3 | 0.2430 | 0.1710 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1530 | 0.1400 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 1.300~1.500 | 1.900~2.800 | 1.800~4.000 | 5.900~6.000 |  |  | 2.900~3.000 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 5~7 | 0~1 | 1~2 |  |  | 2~3 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 70 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  |  | 5th |  |  |  |  |  |  |  |
| ENo | E1186 | E2182 | E2183 | E2184 |  |  | E2185 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1840 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15(D) | 0.2140 | 0.1370 |  |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8(D) | 0.2210 | 0.1440 | 0.1310 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 4(D) | 0.2280 | 0.1510 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| Finish 3(D) | 0.2300 | 0.1530 | 0.1400 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| +1 Finish 8(D) | 0.2390 | 0.1620 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1440 | 0.1310 |  |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4(D) | 0.2460 | 0.1690 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1510 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 3(D) | 0.2480 | 0.1710 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1530 | 0.1400 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 1.100~1.300 | 1.500~2.000 | 1.600~3.100 | 6.000 |  |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 4~5 | 0~1 | 2~3 |  |  | 1~2 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

299

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS | 0.25 |  |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 70 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1186 | E1187 | E1188 | E1189 |  | E1190 |  |  |  |  |  |  |  |
| Roughing | 0.1840 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.2140 | 0.1370 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.2210 | 0.1440 | 0.1310 |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.2280 | 0.1510 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.2300 | 0.1530 | 0.1400 | 0.1310 |  | 0.1300 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2390 | 0.1620 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1440 | 0.1310 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2460 | 0.1690 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1510 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |
| +1 Finish 3 | 0.2480 | 0.1710 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1530 | 0.1400 | 0.1310 |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 1.100~1.300 | 1.500~2.000 | 1.600~3.100 | 6.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 4~5 | 0~1 | 2~3 |  | 1~2 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 80 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1126 | E2122 | E2123 | E2124 |  | E2125 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1820 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15(D) | 0.2140 | 0.1370 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8(D) | 0.2210 | 0.1440 | 0.1310 |  |  |  |  |  |  |  |  |  |  |
| Finish 4(D) | 0.2280 | 0.1510 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |
| Finish 3(D) | 0.2300 | 0.1530 | 0.1400 | 0.1310 |  | 0.1300 |  |  |  |  |  |  |  |
| +1 Finish 8(D) | 0.2390 | 0.1620 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1440 | 0.1310 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4(D) | 0.2460 | 0.1690 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1510 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |
| +1 Finish 3(D) | 0.2480 | 0.1710 |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1530 | 0.1400 | 0.1310 |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.800~1.000 | 1.400~1.900 | 2.100~3.600 | 5.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 4~5 | 0~1 | 2~3 |  | 1~2 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

300

| Unit | Machine |  | Version | Wire |  |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.25 |  |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 80 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  |  | 5th |  |  |  |  |  |  |  |
| ENo | E1126 | E1127 | E1128 | E1129 |  |  | E1130 |  |  |  |  |  |  |  |
| Roughing | 0.1820 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.2140 | 0.1370 |  |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.2210 | 0.1440 | 0.1310 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.2280 | 0.1510 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| Finish 3 | 0.2300 | 0.1530 | 0.1400 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2390 | 0.1620 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1440 | 0.1310 |  |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2460 | 0.1690 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1510 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 3 | 0.2480 | 0.1710 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1530 | 0.1400 | 0.1310 |  |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.800~1.000 | 1.400~1.900 | 2.100~3.600 | 5.000 |  |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 4~5 | 0~1 | 2~3 |  |  | 1~2 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 3~4 |  |  | 2~3 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.38 ~0.50 |  |  | 0.25 ~0.38 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 100 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  |  | 5th |  |  |  |  |  |  |  |
| ENo | E1136 | E2132 | E2133 | E2134 |  |  | E2135 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1800 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15(D) | 0.2130 | 0.1380 |  |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8(D) | 0.2220 | 0.1470 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5(D) | 0.2280 | 0.1530 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| Finish 4(D) | 0.2310 | 0.1560 | 0.1410 | 0.1320 |  |  | 0.1310 |  |  |  |  |  |  |  |
| +1 Finish 8(D) | 0.2480 | 0.1730 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1470 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 5(D) | 0.2540 | 0.1790 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1530 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4(D) | 0.2570 | 0.1820 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1560 | 0.1410 | 0.1320 |  |  | 0.1310 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.550~0.590 | 1.600~1.800 | 1.400~2.600 | 5.000~5.200 |  |  | 5.000~5.200 |  |  |  |  |  |  |  |
| ServoLamp | 3~5 | 6~7 | 3~4 | 4~6 |  |  | 4~6 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 4~5 |  |  | 3~4 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.50 ~0.63 |  |  | 0.38 ~0.50 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

301

| Unit | Machine |  | Version | Wire |  |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.25 |  |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 100 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  |  | 5th |  |  |  |  |  |  |  |
| ENo | E1136 | E1137 | E1138 | E1139 |  |  | E1140 |  |  |  |  |  |  |  |
| Roughing | 0.1800 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.2130 | 0.1380 |  |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.2220 | 0.1470 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5 | 0.2280 | 0.1530 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.2310 | 0.1560 | 0.1410 | 0.1320 |  |  | 0.1310 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2480 | 0.1730 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1470 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 5 | 0.2540 | 0.1790 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1530 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2570 | 0.1820 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1560 | 0.1410 | 0.1320 |  |  | 0.1310 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.550~0.590 | 1.600~1.800 | 1.400~2.600 | 5.000~5.200 |  |  | 5.000~5.200 |  |  |  |  |  |  |  |
| ServoLamp | 3~5 | 6~7 | 3~4 | 4~6 |  |  | 4~6 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 4~5 |  |  | 3~4 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.50 ~0.63 |  |  | 0.38 ~0.50 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 125 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  |  | 5th |  |  |  |  |  |  |  |
| ENo | E1146 | E2142 | E2143 | E2144 |  |  | E2145 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1800 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15(D) | 0.2130 | 0.1380 |  |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8(D) | 0.2220 | 0.1470 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5(D) | 0.2280 | 0.1530 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| Finish 4(D) | 0.2310 | 0.1560 | 0.1410 | 0.1320 |  |  | 0.1310 |  |  |  |  |  |  |  |
| +1 Finish 8(D) | 0.2480 | 0.1730 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1470 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 5(D) | 0.2540 | 0.1790 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1530 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4(D) | 0.2570 | 0.1820 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1560 | 0.1410 | 0.1320 |  |  | 0.1310 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.430~0.470 | 1.300~1.600 | 1.100~2.200 | 4.700~5.100 |  |  | 4.000~4.300 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 6~7 | 3~4 | 3~5 |  |  | 3~5 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 4~5 |  |  | 3~4 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.50 ~0.63 |  |  | 0.38 ~0.50 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

302

| Unit | Machine |  | Version | Wire |  |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.25 |  |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 125 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  |  | 5th |  |  |  |  |  |  |  |
| ENo | E1146 | E1147 | E1148 | E1149 |  |  | E1150 |  |  |  |  |  |  |  |
| Roughing | 0.1800 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.2130 | 0.1380 |  |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.2220 | 0.1470 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5 | 0.2280 | 0.1530 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.2310 | 0.1560 | 0.1410 | 0.1320 |  |  | 0.1310 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2480 | 0.1730 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1470 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 5 | 0.2540 | 0.1790 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1530 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2570 | 0.1820 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1560 | 0.1410 | 0.1320 |  |  | 0.1310 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.430~0.470 | 1.300~1.600 | 1.100~2.200 | 4.700~5.100 |  |  | 4.000~4.300 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 6~7 | 3~4 | 3~5 |  |  | 3~5 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 4~5 |  |  | 3~4 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.50 ~0.63 |  |  | 0.38 ~0.50 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 150 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  |  | 5th |  |  |  |  |  |  |  |
| ENo | E1156 | E2152 | E2153 | E2154 |  |  | E2155 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1800 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15(D) | 0.2130 | 0.1380 |  |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8(D) | 0.2220 | 0.1470 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5(D) | 0.2280 | 0.1530 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| Finish 4(D) | 0.2310 | 0.1560 | 0.1410 | 0.1320 |  |  | 0.1310 |  |  |  |  |  |  |  |
| +1 Finish 8(D) | 0.2480 | 0.1730 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1470 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 5(D) | 0.2540 | 0.1790 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1530 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4(D) | 0.2570 | 0.1820 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1560 | 0.1410 | 0.1320 |  |  | 0.1310 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.300~0.340 | 1.000~1.400 | 0.800~1.900 | 4.400~5.000 |  |  | 3.000~3.300 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 6~7 | 3~4 | 2~4 |  |  | 2~4 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 4~5 |  |  | 3~4 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.50 ~0.63 |  |  | 0.38 ~0.50 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

303

| Unit | Machine |  | Version | Wire |  |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.25 |  |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 150 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  |  | 5th |  |  |  |  |  |  |  |
| ENo | E1156 | E1157 | E1158 | E1159 |  |  | E1160 |  |  |  |  |  |  |  |
| Roughing | 0.1800 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.2130 | 0.1380 |  |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.2220 | 0.1470 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5 | 0.2280 | 0.1530 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.2310 | 0.1560 | 0.1410 | 0.1320 |  |  | 0.1310 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2480 | 0.1730 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1470 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 5 | 0.2540 | 0.1790 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1530 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2570 | 0.1820 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1560 | 0.1410 | 0.1320 |  |  | 0.1310 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.300~0.340 | 1.000~1.400 | 0.800~1.900 | 4.400~5.000 |  |  | 3.000~3.300 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 6~7 | 3~4 | 2~4 |  |  | 2~4 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 4~5 |  |  | 3~4 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.50 ~0.63 |  |  | 0.38 ~0.50 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 200 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  |  | 5th |  |  |  |  |  |  |  |
| ENo | E1176 | E2172 | E2173 | E2174 |  |  | E2175 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1800 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15(D) | 0.2130 | 0.1380 |  |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8(D) | 0.2220 | 0.1470 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5(D) | 0.2280 | 0.1530 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| Finish 4(D) | 0.2310 | 0.1560 | 0.1410 | 0.1320 |  |  | 0.1310 |  |  |  |  |  |  |  |
| +1 Finish 8(D) | 0.2480 | 0.1730 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1470 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 5(D) | 0.2540 | 0.1790 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1530 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4(D) | 0.2570 | 0.1820 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1560 | 0.1410 | 0.1320 |  |  | 0.1310 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.210~0.250 | 0.700~1.000 | 0.500~1.500 | 2.400~2.600 |  |  | 2.400~2.500 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 6~7 | 3~4 | 2~4 |  |  | 1~3 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 4~5 |  |  | 3~4 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.50 ~0.63 |  |  | 0.38 ~0.50 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

304

| Unit | Machine |  | Version | Wire |  |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.25 |  |  |  | St |  | Both Away |  |  |
| Thickness (mm) | 200 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  |  | 5th |  |  |  |  |  |  |  |
| ENo | E1176 | E1177 | E1178 | E1179 |  |  | E1180 |  |  |  |  |  |  |  |
| Roughing | 0.1800 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.2130 | 0.1380 |  |  |  |  |  |  |  |  |  |  |  |  |
| Finish 8 | 0.2220 | 0.1470 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5 | 0.2280 | 0.1530 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.2310 | 0.1560 | 0.1410 | 0.1320 |  |  | 0.1310 |  |  |  |  |  |  |  |
| +1 Finish 8 | 0.2480 | 0.1730 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1470 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 5 | 0.2540 | 0.1790 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1530 | 0.1380 | 0.1290 |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2570 | 0.1820 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1560 | 0.1410 | 0.1320 |  |  | 0.1310 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.210~0.250 | 0.700~1.000 | 0.500~1.500 | 2.400~2.600 |  |  | 2.400~2.500 |  |  |  |  |  |  |  |
| ServoLamp | 1~3 | 6~7 | 3~4 | 2~4 |  |  | 1~3 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 7~8 | 4~5 |  |  | 3~4 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.92 ~1.06 | 0.50 ~0.63 |  |  | 0.38 ~0.50 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

| Unit | : | Metric |
| --- | --- | --- |
| Machine | : | W32FB,W53FB(EW100A) |
| Version | : | 8 |
| Wire Type | : | BS |
| Wire Diameter | : | 0.25 |
| Material | : Cu |  |
| MC. Method | : Both Away |  |
| W. Thickness | : 5~60 |  |
| Angle | : 0~0 |  |
| Nozzle Type | : Laminar |  |
| Nozzle Position | : Away |  |
| M. Condition | : Standard |  |

353

| Unit | Machine |  | Version |  | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.25 |  |  |  | Cu |  | Both Away |  |  |
| Thickness (mm) | 5 |  |  |  |  |  | 10 |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  | 0 |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd |  |  |  | 1st |  |  | 2nd | 3rd |  |  |  |
| ENo | E1634 | E1635 | E1636 |  |  |  | E1644 |  |  | E1645 | E1646 |  |  |  |
| Roughing | 0.1660 |  |  |  |  |  | 0.1750 |  |  |  |  |  |  |  |
| 2nd 15 | 0.1870 | 0.1330 |  |  |  |  | 0.1930 |  |  | 0.1350 |  |  |  |  |
| Finish 3 | 0.1930 | 0.1390 | 0.1320 |  |  |  | 0.1980 |  |  | 0.1400 | 0.1320 |  |  |  |
| +1 Finish 3 | 0.2130 | 0.1590 |  |  |  |  | 0.2180 |  |  | 0.1600 |  |  |  |  |
|  |  | 0.1390 | 0.1320 |  |  |  |  |  |  | 0.1400 | 0.1320 |  |  |  |
| HValue | V-Corner |  |  |  |  |  | V-Corner |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - |  |  |  | - |  |  | - | - |  |  |  |
| PressureL (MPa) | - | - | - |  |  |  | - |  |  | - | - |  |  |  |
| Rem. R. (mm/min) | 9.500~11.500 | 16.700~20.000 | 20.000 |  |  |  | 7.900~9.700 |  |  | 17.700~20.000 | 20.000 |  |  |  |
| ServoLamp | 6~8 | 8~9 | 9~10 |  |  |  | 6~8 |  |  | 9~10 | 7 |  |  |  |
| SparkLamp | 12 | 12 | - |  |  |  | 12 |  |  | 12 | - |  |  |  |
| SF1 (µmRz) | 18 | 10~11 | 2~3 |  |  |  | 18 |  |  | 10~11 | 2~3 |  |  |  |
| SF2 (µmRa) | 2.47 | 1.32 ~1.45 | 0.25 ~0.38 |  |  |  | 2.47 |  |  | 1.32 ~1.45 | 0.25 ~0.38 |  |  |  |
| AR (mm) | - | - | - |  |  |  | - |  |  | - | - |  |  |  |
| Thickness (mm) | 15 |  |  |  |  |  | 20 |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  | 0 |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd |  |  |  | 1st |  |  | 2nd | 3rd |  |  |  |
| ENo | E1654 | E1655 | E1656 |  |  |  | E1664 |  |  | E1665 | E1666 |  |  |  |
| Roughing | 0.1800 |  |  |  |  |  | 0.1800 |  |  |  |  |  |  |  |
| 2nd 15 | 0.1980 | 0.1350 |  |  |  |  | 0.1960 |  |  | 0.1350 |  |  |  |  |
| Finish 4 | 0.2040 | 0.1410 | 0.1330 |  |  |  | 0.2030 |  |  | 0.1420 | 0.1330 |  |  |  |
| +1 Finish 4 | 0.2240 | 0.1610 |  |  |  |  | 0.2230 |  |  | 0.1620 |  |  |  |  |
|  |  | 0.1410 | 0.1330 |  |  |  |  |  |  | 0.1420 | 0.1330 |  |  |  |
| HValue | V-Corner |  |  |  |  |  | V-Corner |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - |  |  |  | - |  |  | - | - |  |  |  |
| PressureL (MPa) | - | - | - |  |  |  | - |  |  | - | - |  |  |  |
| Rem. R. (mm/min) | 5.700~6.900 | 12.000~14.600 | 20.000 |  |  |  | 4.900~5.900 |  |  | 10.800~13.200 | 15.000 |  |  |  |
| ServoLamp | 6~8 | 9~10 | 6 |  |  |  | 5~7 |  |  | 9~10 | 5 |  |  |  |
| SparkLamp | 12 | 12 | - |  |  |  | 12 |  |  | 12 | - |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 3~4 |  |  |  | 20 |  |  | 10~12 | 3~4 |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.38 ~0.50 |  |  |  | 2.74 |  |  | 1.32 ~1.64 | 0.38 ~0.50 |  |  |  |
| AR (mm) | - | - | - |  |  |  | - |  |  | - | - |  |  |  |
| Thickness (mm) | 25 |  |  |  |  |  | 30 |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  | 0 |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd |  |  |  | 1st |  |  | 2nd | 3rd |  |  |  |
| ENo | E1674 | E1675 | E1676 |  |  |  | E1684 |  |  | E1685 | E1686 |  |  |  |
| Roughing | 0.1850 |  |  |  |  |  | 0.1880 |  |  |  |  |  |  |  |
| 2nd 15 | 0.2010 | 0.1350 |  |  |  |  | 0.2060 |  |  | 0.1370 |  |  |  |  |
| Finish 4 | 0.2080 | 0.1420 | 0.1340 |  |  |  | 0.2130 |  |  | 0.1440 | 0.1340 |  |  |  |
| +1 Finish 4 | 0.2280 | 0.1620 |  |  |  |  | 0.2330 |  |  | 0.1640 |  |  |  |  |
|  |  | 0.1420 | 0.1340 |  |  |  |  |  |  | 0.1440 | 0.1340 |  |  |  |
| HValue | V-Corner |  |  |  |  |  | V-Corner |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - |  |  |  | - |  |  | - | - |  |  |  |
| PressureL (MPa) | - | - | - |  |  |  | - |  |  | - | - |  |  |  |
| Rem. R. (mm/min) | 3.800~4.600 | 7.800~9.600 | 15.000 |  |  |  | 3.200~4.000 |  |  | 5.800~7.000 | 10.000 |  |  |  |
| ServoLamp | 6~7 | 9~10 | 4 |  |  |  | 6~7 |  |  | 9~10 | 4 |  |  |  |
| SparkLamp | 12 | 12 | - |  |  |  | 12 |  |  | 12 | - |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 3~4 |  |  |  | 20 |  |  | 10~12 | 3~4 |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.38 ~0.50 |  |  |  | 2.74 |  |  | 1.32 ~1.64 | 0.38 ~0.50 |  |  |  |
| AR (mm) | - | - | - |  |  |  | - |  |  | - | - |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

354

| Unit | Machine |  | Version |  | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS |  | 0.25 |  |  |  | Cu |  | Both Away |  |  |
| Thickness (mm) | 40 |  |  |  |  |  | 50 |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  | 0 |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd |  |  |  | 1st |  |  | 2nd | 3rd |  |  |  |
| ENo | E1694 | E1695 | E1696 |  |  |  | E1704 |  |  | E1705 | E1706 |  |  |  |
| Roughing | 0.1930 |  |  |  |  |  | 0.1960 |  |  |  |  |  |  |  |
| 2nd 15 | 0.2120 | 0.1390 |  |  |  |  | 0.2160 |  |  | 0.1410 |  |  |  |  |
| Finish 4 | 0.2180 | 0.1450 | 0.1340 |  |  |  | 0.2210 |  |  | 0.1460 | 0.1340 |  |  |  |
| +1 Finish 4 | 0.2380 | 0.1650 |  |  |  |  | 0.2410 |  |  | 0.1660 |  |  |  |  |
|  |  | 0.1450 | 0.1340 |  |  |  |  |  |  | 0.1460 | 0.1340 |  |  |  |
| HValue | V-Corner |  |  |  |  |  | V-Corner |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - |  |  |  | - |  |  | - | - |  |  |  |
| PressureL (MPa) | - | - | - |  |  |  | - |  |  | - | - |  |  |  |
| Rem. R. (mm/min) | 2.300~2.900 | 4.500~5.500 | 10.000 |  |  |  | 1.800~2.200 |  |  | 3.400~4.200 | 10.000 |  |  |  |
| ServoLamp | 5~7 | 9~10 | 3 |  |  |  | 6~7 |  |  | 9~10 | 4 |  |  |  |
| SparkLamp | 12 | 12 | - |  |  |  | 12 |  |  | 12 | - |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 3~4 |  |  |  | 20 |  |  | 10~12 | 3~4 |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.38 ~0.50 |  |  |  | 2.74 |  |  | 1.32 ~1.64 | 0.38 ~0.50 |  |  |  |
| AR (mm) | - | - | - |  |  |  | - |  |  | - | - |  |  |  |
| Thickness (mm) | 60 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd |  |  |  |  |  |  |  |  |  |  |  |
| ENo | E1714 | E1715 | E1716 |  |  |  |  |  |  |  |  |  |  |  |
| Roughing | 0.2010 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 15 | 0.2200 | 0.1410 |  |  |  |  |  |  |  |  |  |  |  |  |
| Finish 4 | 0.2260 | 0.1470 | 0.1340 |  |  |  |  |  |  |  |  |  |  |  |
| +1 Finish 4 | 0.2460 | 0.1670 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  | 0.1470 | 0.1340 |  |  |  |  |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - |  |  |  |  |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - |  |  |  |  |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 1.400~1.800 | 2.700~3.300 | 10.000 |  |  |  |  |  |  |  |  |  |  |  |
| ServoLamp | 5~7 | 9~10 | 3 |  |  |  |  |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | - |  |  |  |  |  |  |  |  |  |  |  |
| SF1 (µmRz) | 20 | 10~12 | 3~4 |  |  |  |  |  |  |  |  |  |  |  |
| SF2 (µmRa) | 2.74 | 1.32 ~1.64 | 0.38 ~0.50 |  |  |  |  |  |  |  |  |  |  |  |
| AR (mm) | - | - | - |  |  |  |  |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

355

| Unit | : | Metric |
| --- | --- | --- |
| Machine | : | W32FB,W53FB(EW100A) |
| Version | : | 8 |
| Wire Type | : | BS |
| Wire Diameter | : | 0.25 |
| Material | : WC |  |
| MC. Method | : Both Away |  |
| W. Thickness | : 5~60 |  |
| Angle | : 0~0 |  |
| Nozzle Type | : Laminar |  |
| Nozzle Position | : Away |  |
| M. Condition | : Standard |  |

371

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS | 0.25 |  |  |  | WC |  | Both Away |  |  |
| Thickness (mm) | 5 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1436 | E3437 | E3438 | E3439 |  | E3440 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1560 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10(D) | 0.1860 | 0.1350 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5(D) | 0.1940 | 0.1430 | 0.1310 |  |  |  |  |  |  |  |  |  |  |
| Finish 2(D) | 0.1990 | 0.1480 | 0.1360 | 0.1300 |  |  |  |  |  |  |  |  |  |
| Finish 1.5(D) | 0.2010 | 0.1500 | 0.1380 | 0.1320 |  | 0.1290 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 4.100~4.400 | 4.500~5.500 | 8.000~9.000 | 8.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 3~6 | 7~9 | 1~3 | 6~8 |  | 5~7 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 5 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1436 | E1437 | E1438 | E1439 |  | E1440 |  |  |  |  |  |  |  |
| Roughing | 0.1560 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10 | 0.1860 | 0.1350 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5 | 0.1940 | 0.1430 | 0.1310 |  |  |  |  |  |  |  |  |  |  |
| Finish 2 | 0.1990 | 0.1480 | 0.1360 | 0.1300 |  |  |  |  |  |  |  |  |  |
| Finish 1.5 | 0.2010 | 0.1500 | 0.1380 | 0.1320 |  | 0.1290 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 4.100~4.400 | 6.000~7.000 | 8.000~9.000 | 8.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 3~6 | 7~9 | 1~3 | 6~8 |  | 5~7 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 10 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1446 | E3447 | E3448 | E3449 |  | E3450 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1570 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10(D) | 0.1880 | 0.1360 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5(D) | 0.1950 | 0.1430 | 0.1320 |  |  |  |  |  |  |  |  |  |  |
| Finish 2(D) | 0.2000 | 0.1480 | 0.1370 | 0.1320 |  |  |  |  |  |  |  |  |  |
| Finish 1.5(D) | 0.2010 | 0.1490 | 0.1380 | 0.1330 |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 3.000~3.400 | 3.500~4.500 | 5.000~6.000 | 6.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 3~6 | 6~8 | 1~3 | 9~11 |  | 8~10 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

372

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS | 0.25 |  |  |  | WC |  | Both Away |  |  |
| Thickness (mm) | 10 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1446 | E1447 | E1448 | E1449 |  | E1450 |  |  |  |  |  |  |  |
| Roughing | 0.1570 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10 | 0.1880 | 0.1360 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5 | 0.1950 | 0.1430 | 0.1320 |  |  |  |  |  |  |  |  |  |  |
| Finish 2 | 0.2000 | 0.1480 | 0.1370 | 0.1320 |  |  |  |  |  |  |  |  |  |
| Finish 1.5 | 0.2010 | 0.1490 | 0.1380 | 0.1330 |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 3.000~3.400 | 4.500~5.500 | 5.000~6.000 | 6.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 3~6 | 6~8 | 1~3 | 9~11 |  | 8~10 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 15 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1456 | E3457 | E3458 | E3459 |  | E3460 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1580 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10(D) | 0.1850 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5(D) | 0.1930 | 0.1400 | 0.1330 |  |  |  |  |  |  |  |  |  |  |
| Finish 2(D) | 0.1970 | 0.1440 | 0.1370 | 0.1320 |  |  |  |  |  |  |  |  |  |
| Finish 1.5(D) | 0.1980 | 0.1450 | 0.1380 | 0.1330 |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 2.200~2.600 | 3.000~4.000 | 4.000~5.000 | 5.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 3~5 | 7~9 | 1~3 | 7~9 |  | 6~8 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 15 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1456 | E1457 | E1458 | E1459 |  | E1460 |  |  |  |  |  |  |  |
| Roughing | 0.1580 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10 | 0.1850 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5 | 0.1930 | 0.1400 | 0.1330 |  |  |  |  |  |  |  |  |  |  |
| Finish 2 | 0.1970 | 0.1440 | 0.1370 | 0.1320 |  |  |  |  |  |  |  |  |  |
| Finish 1.5 | 0.1980 | 0.1450 | 0.1380 | 0.1330 |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 2.200~2.600 | 3.500~4.500 | 4.000~5.000 | 5.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 3~5 | 7~9 | 1~3 | 7~9 |  | 6~8 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

373

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS | 0.25 |  |  |  | WC |  | Both Away |  |  |
| Thickness (mm) | 20 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1466 | E3467 | E3468 | E3469 |  | E3470 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1620 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10(D) | 0.1890 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5(D) | 0.1970 | 0.1400 | 0.1330 |  |  |  |  |  |  |  |  |  |  |
| Finish 2(D) | 0.2010 | 0.1440 | 0.1370 | 0.1310 |  |  |  |  |  |  |  |  |  |
| Finish 1.5(D) | 0.2020 | 0.1450 | 0.1380 | 0.1320 |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 1.900~2.300 | 2.500~3.500 | 3.500~4.500 | 5.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 6~8 | 1~3 | 6~8 |  | 4~6 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 20 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1466 | E1467 | E1468 | E1469 |  | E1470 |  |  |  |  |  |  |  |
| Roughing | 0.1620 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10 | 0.1890 | 0.1320 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5 | 0.1970 | 0.1400 | 0.1330 |  |  |  |  |  |  |  |  |  |  |
| Finish 2 | 0.2010 | 0.1440 | 0.1370 | 0.1310 |  |  |  |  |  |  |  |  |  |
| Finish 1.5 | 0.2020 | 0.1450 | 0.1380 | 0.1320 |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 1.900~2.300 | 3.000~4.000 | 3.500~4.500 | 5.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 6~8 | 1~3 | 6~8 |  | 4~6 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 25 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1476 | E3477 | E3478 | E3479 |  | E3480 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1650 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10(D) | 0.1910 | 0.1310 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5(D) | 0.1990 | 0.1390 | 0.1330 |  |  |  |  |  |  |  |  |  |  |
| Finish 2(D) | 0.2030 | 0.1430 | 0.1370 | 0.1320 |  |  |  |  |  |  |  |  |  |
| Finish 1.5(D) | 0.2040 | 0.1440 | 0.1380 | 0.1330 |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 1.600~2.000 | 2.200~3.200 | 3.000~4.000 | 4.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 3~5 | 6~8 | 1~3 | 5~7 |  | 4~6 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

374

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS | 0.25 |  |  |  | WC |  | Both Away |  |  |
| Thickness (mm) | 25 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1476 | E1477 | E1478 | E1479 |  | E1480 |  |  |  |  |  |  |  |
| Roughing | 0.1650 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10 | 0.1910 | 0.1310 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5 | 0.1990 | 0.1390 | 0.1330 |  |  |  |  |  |  |  |  |  |  |
| Finish 2 | 0.2030 | 0.1430 | 0.1370 | 0.1320 |  |  |  |  |  |  |  |  |  |
| Finish 1.5 | 0.2040 | 0.1440 | 0.1380 | 0.1330 |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 1.600~2.000 | 2.500~3.500 | 3.000~4.000 | 4.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 3~5 | 6~8 | 1~3 | 5~7 |  | 4~6 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 30 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1486 | E3487 | E3488 | E3489 |  | E3490 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1680 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10(D) | 0.1960 | 0.1330 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5(D) | 0.2040 | 0.1410 | 0.1330 |  |  |  |  |  |  |  |  |  |  |
| Finish 2(D) | 0.2080 | 0.1450 | 0.1370 | 0.1320 |  |  |  |  |  |  |  |  |  |
| Finish 1.5(D) | 0.2090 | 0.1460 | 0.1380 | 0.1330 |  | 0.1310 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 1.200~1.600 | 1.700~2.700 | 2.500~3.500 | 4.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 3~5 | 5~7 | 1~3 | 4~6 |  | 2~4 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 30 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1486 | E1487 | E1488 | E1489 |  | E1490 |  |  |  |  |  |  |  |
| Roughing | 0.1680 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10 | 0.1960 | 0.1330 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5 | 0.2040 | 0.1410 | 0.1330 |  |  |  |  |  |  |  |  |  |  |
| Finish 2 | 0.2080 | 0.1450 | 0.1370 | 0.1320 |  |  |  |  |  |  |  |  |  |
| Finish 1.5 | 0.2090 | 0.1460 | 0.1380 | 0.1330 |  | 0.1310 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 1.200~1.600 | 2.000~3.000 | 2.500~3.500 | 4.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 3~5 | 5~7 | 1~3 | 4~6 |  | 2~4 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

375

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS | 0.25 |  |  |  | WC |  | Both Away |  |  |
| Thickness (mm) | 40 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1496 | E3497 | E3498 | E3499 |  | E3500 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1730 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10(D) | 0.2030 | 0.1340 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5(D) | 0.2110 | 0.1420 | 0.1330 |  |  |  |  |  |  |  |  |  |  |
| Finish 2(D) | 0.2150 | 0.1460 | 0.1370 | 0.1310 |  |  |  |  |  |  |  |  |  |
| Finish 1.5(D) | 0.2160 | 0.1470 | 0.1380 | 0.1320 |  | 0.1310 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.800~1.200 | 1.200~2.200 | 1.800~2.800 | 4.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 5~7 | 1~3 | 3~5 |  | 1~3 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 40 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1496 | E1497 | E1498 | E1499 |  | E1500 |  |  |  |  |  |  |  |
| Roughing | 0.1730 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10 | 0.2030 | 0.1340 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5 | 0.2110 | 0.1420 | 0.1330 |  |  |  |  |  |  |  |  |  |  |
| Finish 2 | 0.2150 | 0.1460 | 0.1370 | 0.1310 |  |  |  |  |  |  |  |  |  |
| Finish 1.5 | 0.2160 | 0.1470 | 0.1380 | 0.1320 |  | 0.1310 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.800~1.200 | 1.500~2.500 | 1.800~2.800 | 4.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 5~7 | 1~3 | 3~5 |  | 1~3 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 50 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1506 | E3507 | E3508 | E3509 |  | E3510 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1730 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10(D) | 0.2010 | 0.1330 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5(D) | 0.2090 | 0.1410 | 0.1330 |  |  |  |  |  |  |  |  |  |  |
| Finish 2(D) | 0.2140 | 0.1460 | 0.1380 | 0.1320 |  |  |  |  |  |  |  |  |  |
| Finish 1.5(D) | 0.2150 | 0.1470 | 0.1390 | 0.1330 |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.650~1.050 | 1.300~2.300 | 1.500~2.500 | 4.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 6~8 | 0~2 | 3~5 |  | 1~3 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.

376

| Unit | Machine |  | Version | Wire |  |  |  | Material |  | MC. Method |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Metric | W32FB,W53FB(EW100A) |  | 8 | BS | 0.25 |  |  |  | WC |  | Both Away |  |  |
| Thickness (mm) | 50 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1506 | E1507 | E1508 | E1509 |  | E1510 |  |  |  |  |  |  |  |
| Roughing | 0.1730 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10 | 0.2010 | 0.1330 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5 | 0.2090 | 0.1410 | 0.1330 |  |  |  |  |  |  |  |  |  |  |
| Finish 2 | 0.2140 | 0.1460 | 0.1380 | 0.1320 |  |  |  |  |  |  |  |  |  |
| Finish 1.5 | 0.2150 | 0.1470 | 0.1390 | 0.1330 |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.650~1.050 | 1.300~2.300 | 1.500~2.500 | 4.000 |  | 3.000 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 6~8 | 0~2 | 3~5 |  | 1~3 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 60 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1516 | E3517 | E3518 | E3519 |  | E3520 |  |  |  |  |  |  |  |
| Roughing(D) | 0.1800 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10(D) | 0.2080 | 0.1340 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5(D) | 0.2160 | 0.1420 | 0.1330 |  |  |  |  |  |  |  |  |  |  |
| Finish 2(D) | 0.2200 | 0.1460 | 0.1370 | 0.1310 |  |  |  |  |  |  |  |  |  |
| Finish 1.5(D) | 0.2210 | 0.1470 | 0.1380 | 0.1320 |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.400~0.600 | 0.700~1.700 | 1.000~2.000 | 3.000 |  | 2.500 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 5~7 | 1~3 | 2~4 |  | 6~8 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Thickness (mm) | 60 |  |  |  |  |  |  |  |  |  |  |  |  |
| Angle (degree) | 0 |  |  |  |  |  |  |  |  |  |  |  |  |
| Process | 1st | 2nd | 3rd | 4th |  | 5th |  |  |  |  |  |  |  |
| ENo | E1516 | E1517 | E1518 | E1519 |  | E1520 |  |  |  |  |  |  |  |
| Roughing | 0.1800 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2nd 10 | 0.2080 | 0.1340 |  |  |  |  |  |  |  |  |  |  |  |
| Finish 5 | 0.2160 | 0.1420 | 0.1330 |  |  |  |  |  |  |  |  |  |  |
| Finish 2 | 0.2200 | 0.1460 | 0.1370 | 0.1310 |  |  |  |  |  |  |  |  |  |
| Finish 1.5 | 0.2210 | 0.1470 | 0.1380 | 0.1320 |  | 0.1300 |  |  |  |  |  |  |  |
| HValue | V-Corner |  |  |  |  |  |  |  |  |  |  |  |  |
| PressureU (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| PressureL (MPa) | - | - | - | - |  | - |  |  |  |  |  |  |  |
| Rem. R. (mm/min) | 0.400~0.600 | 1.000~2.000 | 1.000~2.000 | 3.000 |  | 2.500 |  |  |  |  |  |  |  |
| ServoLamp | 2~4 | 5~7 | 1~3 | 2~4 |  | 6~8 |  |  |  |  |  |  |  |
| SparkLamp | 12 | 12 | 12 | - |  | - |  |  |  |  |  |  |  |
| SF1 (µmRz) | 10 | 7 | 5 | 1.5~2 |  | 1~1.5 |  |  |  |  |  |  |  |
| SF2 (µmRa) | 1.32 | 0.92 | 0.63 | 0.19 ~0.25 |  | 0.13 ~0.19 |  |  |  |  |  |  |  |
| AR (mm) | - | - | - | - |  | - |  |  |  |  |  |  |  |

Note: HValue, PressureU and PressureL are only applicable for Roughing.